Euco QWIKjoint UVR 65

Joint Filler

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 1, 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 1:	GENERAL

1.__	APPLICATOR QUALIFICATIONS

A.	Experienced applicator who has successfully completed 5 jobs of similar	size and scope in the prior 5 years.

1.__	MOCK UP

A.	Applicator shall apply 10 lineal feet of joint filler.

B.	The Owner, franchisee, or their representative will view the samples and the Work will not proceed until a sample has been approved.

C.	Once approved use the same procedures for the Work.

1.__	PRE-JOB MEETING

A.	Prior to the start of concrete placement Contractor shall conduct a meeting to review the required methods and procedures to achieve the required joint filling. Contractor shall send a meeting agenda to all attendees 20 days prior to the scheduled date of the meeting.

B.	The Contractor shall require responsible representatives of every party concerned with the concreting work to attend the meeting, including but not limited to the following: Contractor’s superintendent, joint filler applicator, and owner’s representative.

C.	Minutes of the meeting shall be recorded, typed, and distributed by the Contractor to all concerned parties, including but not limited to the owner’s representative and all attendees within 5 days of the meeting.

PART 2:	PRODUCTS

2.__	JOINT FILLER

A.	White, light reflective, UV resistant, fast setting, semi-rigid polyurea joint filler with minimum Shore A Hardness between 64 and 70 per ASTM D 2240.

1.	Product: “Euco QWIKjoint UVR 65” by the Euclid Chemical Company

2.	Color to be selected from manufacturer’s standard colors.

PART 3:	EXECUTION

3.__	JOINT FILLER INSTALLATION

A.	Concrete substrate shall be structurally sound and free from deteriorated concrete, dust, dirt, paint, oil, efflorescence, laitance, and other contaminants.

B.	All joint facings shall possess an open surface texture. This is typically done by running a saw blade or grinder down each side of the joint to expose fresh concrete.

C.	Do not use backer rod, sand, or other fill material. Joint Filler shall be full depth. A very thin sand layer is acceptable to help prevent the Joint Filler from flowing into the substrate.

D.	Blow joints clean using un-oiled air.

E.	Mix Joint Filler per manufacturer’s recommendations.

F.	Fill joint full depth and overfill slightly.

G. 	Shave overfilled material to flush with the surface. (Typically in 1 hour, but no longer than 24 hours.)

H.	Other trades shall avoid walking and driving through uncured Joint Filler.